A close-up of some grass

Description automatically generated

Specification Sheet: Imperial 19

Imperial is a stunning grass which is soft and springy to touch. It has a superb multitone 35mm pile with a dense brown thatch. Imperial has a memory pile to give you a lush lawn throughout the year.

Imperial 19 – 35mm Pile Height

* Manufacturer – Nomow Ltd
  + Web: [www.nomow.co.uk](http://www.nomow.co.uk/)
  + Tel: 0800 587 0380
  + Product reference: Imperial 19

|  |  |
| --- | --- |
| **Fibre** | 65 % PE / 35 % PP straight / curled |
| **Fibre Shape** | |
| **Production Method** | Tufting |
| **Gauge** | 3/8” |
| **#stitches / lm** | ca. 175st/lm |
| **#tufts / m²** | ca. 18375 / m² |
| **Pile Height** | ca. 35 mm |
| **Pile Weight** | ca. 1407 g / m² |
| **Total Weight** | ca. 2377 g / m² |
| **Tuft Cloth** | Polypropylenewoven, ca. 170 g / m² |
| **Backing** | Latex, ca. 800 g / m² |
| **Roll width** | 400 cm |
| **Roll length** | 25 m |
| **Colour Fastness** | Scale 7 (DIN 54004) |
| **UV-Stability** | > 3,000 hours UV-A |
| **Chlorine Resistance** | 4 –5 (DIN 54019) |
| **Resistance to sea water** | 4 –5 (DIN 54007) |

*“Nomow has the right to alter each product specification in order to improve the artificial grass according to the newest technological applications. Nomow is not legally liable in case of non-compliance with these mentioned specifications.”*