

Specification Sheet: Rainbow Range

Our Rainbow Range includes a variety of bright, fun colours that are perfect for creating designs and themed gardens and playareas. It is still a tufted grass with a short pile giving it that ‘grass’ look.

Rainbow Range – 24mm Pile Height

* Manufacturer – Nomow Ltd
	+ Web: [www.nomow.co.uk](http://www.nomow.co.uk/)
	+ Tel: 0800 587 0380
	+ Product reference: Rainbow Range

|  |  |
| --- | --- |
| **Fibre** | 65% PE / 35% PP |
| **Production Method** | Tufting |
| **Gauge** | 3/8” |
| **# stitches / lm** | ca. 160 / lm |
| **# tufts / m²** | ca. 16,800 / m² |
| **Pile Height** | ca. 24 mm |
| **Pile Weight** | ca. 1,196 g / m² |
| **Total Weight** | ca. 2,166 g / m² |
| **Tuft Cloth** | Polypropylene woven, ca. 170 g / m² |
| **Backing** | Latex, ca. 800 g / m² |
| **Roll width** | 400 cm |
| **Colour Fastness** | Scale 7 (DIN 54004) |
| **UV-Stability** | > 3,000 hours UV-A |
| **Chlorine Resistance** | 4 – 5 (DIN 54019) |
| **Resistance to sea water** | 4 – 5 (DIN 54007) |

*“Nomow has the right to alter each product specification in order to improve the artificial grass according to the newest technological applications. Nomow is not legally liable in case of non-compliance with these mentioned specifications.”*