Close-up of grass in a field

Description automatically generated with medium confidence

Specification Sheet: Luxury Plus 2020

A silky-smooth grass combined with density and softness. The four colours gives a truly natural appearance and is highly recommended for both gardens and landscaping.

Luxury Plus 2020 – 40mm Pile Height

* Manufacturer – Nomow Ltd
  + Web: [www.nomow.co.uk](http://www.nomow.co.uk/)
  + Tel: 0800 587 0380
  + Product reference: Luxury Plus 2020

**Fibre**: 75% PE /25% PE straight / curled

**Fibre Shape**: W-shape + C Rib + Xtra Spine Technology

**Pile height**: ca. 40mm

**# Stitches**: ca. 23/ 10 cm

**Production**: Tufting

**Gauge**: 3/8”

**# Tufts**: ca. 24,150 / m²

**Pile weight**: ca. 1,868 gr / m²

**Total weight**: ca. 2,838 gr / m²

**Tuft cloth**: Polypropylene woven, ca. 170 gr / m²

**Backing**: Pre coat, ca. 800 gr / m²

**Roll width**: 400 cm

**Roll length**: ±25 m

**UV Stability**: > 3,000 hours UV-A │6,000 hours XENON

**Light fastness**: Scale 7 (DIN 54004)

**Chlorine resistance**: 4 –5 (DIN 54019)

**Resistance to sea water**: 4 –5 (DIN 54007)

*“Nomow has the right to alter each product specification in order to improve the artificial grass according to the newest technological applications. Nomow is not legally liable in case of non-compliance with these mentioned specifications.”*